UNIVERSITY OF CALIFORNIA

College of Engineering

Department of Electrical Engineering and Computer Sciences

EECS 130 							      Professor Chenming Hu

Spring 2006

HOMEWORK SET NO. 7

Due: Friday, 10th March, 2006

Problem 1:

If we decrease the substrate doping concentration, how will the following parameters be affected?  (Please indicate your answer by putting a mark, X, in the correct square.)  Write down any relevant equation and explain briefly how you obtain the answer (a few words or one sentence).  Assume the gate material is     N+-poly and the body is P-type.

|  | Parameters | Increase | Decrease | Unchanged |
| --- | --- | --- | --- | --- |
| A | Accumulation Region Capacitance |  |  |  |
| B | Flat-band Voltage, Vfb |  |  |  |
| C | Depletion Region Capacitance |  |  |  |
| D | Threshold Voltage, Vt |  |  |  |
| E | Inversion Region Capacitance |  |  |  |

Problem 2:

The oxide thickness (Tox) and the doping concentration (Na or Nd) of the silicon substrate can be determined using the high-frequency C-V data shown below for an MOS structure.

- Identify the regions of accumulation, depletion and inversion in the substrate corresponding to this C-V curve.  What is the doping type of the semiconductor?

- If the maximum capacitance of the structure C0 (which is equal to Cox(Area) is 82 pF and the gate area is   4.75(10-3 cm2, what is the value of Tox?

- Determine the concentration in the silicon substrate.  Assume a uniform doping concentration.

Problem 3:

Consider the C-V curve of a MOS capacitor in the figure (the solid line). The

capacitor area is 6400 (m2.  C0 = 45 pF and C1 = 5.6 pF.

If, due to the oxide fixed charge, the C-V curve shifted from the solid line to the dashed line with (V = 0.05V, what is the charge polarity and the area density     (C/cm2) of the oxide fixed charge?

Problem 4:

(a)	Derive Eq.5.8.1.

- Derive an expression for the voltage drop in the poly-depletion region, i.e. the band bending in the poly-Si gate, (s.  Assume that the electric field inside the oxide ,(ox, is known.

- Continue from (b) and express (poly in terms of Vg, not (ox.  Assume surface in version, i.e. Vg ( Vt.  Other usual MOS parameters such as Vfb, Tox, (B may also appear.  Hint: Vg = Vfb + Vox + 2(B + (poly.

- Using the result of (c), find an expression for Wdpoly in terms of Vg, not (ox.

##### For part (e), (f), and (g), assume Tox = 2nm, Na = 1017cm-3, Nd = 6(1019cm-3 (for N+-poly-gate), and Vg = 1.5V.

- Evaluate (poly and Wdpoly.

- Calculate Vt using Eq. 5.4.3.  (The poly-depletion effect maybe ignored in Vt calculation because (ox is very low at Vg=Vt.)  Then, using (poly from part (e) in Eq. 5.8.3, find Qinv.

- Calculate Qinv = Coxe(Vg-Vt) with Coxe given by Eq. 5.8.2.

Discussion:

Eq. 5.8.2 is correct for a small signal capacitor. In this case,

where C and Q are functions of Vg.  Hence, solving the integral above will not yield the same result you obtained for part (f) since C varies with Vg due to the poly-depletion effect.  The answer for part (f) is the correct value for Qinv.

# Text boxes

0

2

4

-2

-4

-6

-8

-12

-10

0.2

0.4

0.6

0.8

1.0

C/C0

High frequency

(V

Vg

Cox

C1